# South Dakota BOR

South Dakota State University

## Residence Hall Mattress Specification

QUANTITY - 75

We reserve the right to request a sample of the product before committing to order.

Product: Firmness Foam Mattress

- Mattress shall be fire-retardant per Federal Specification DOC-FF-4 72 and California Technical Bulletin #117.   Shall be dual foam with fire retardant outer cover.  Each Mattress is to be packed in individual polyethylene bags.

- Mattress shall be of the following nominal dimensions:

36” Width x 80” Length

Materials:

DUAL FIRMNESS FOAM MATTRESS

- Topper: 5 Zone 2-inch convoluted high density plush topper

- Core: 4-inch firm high density foam core

- Components bond together by a non-toxic water-based adhesive.

- Cover: XP FR – FB 210Denier poly urethane coated nylon ticking with laminated FR Barrier

- Inverted seam lock stitch construction

- FR thread (fire retardant)

- All safety testing done by UL Laboratories

- Mattress conforms to CFR 1632

- Mattress conforms to new CPSC 16 CFR 1633

- Mattress conforms to BFD IX-11 BC

- Mattress conforms to California Bureau of Home Furnishings Technical Bulletin 129 “Flammability Test Procedure for Mattresses for use in Public Buildings.”

- Entire mattress must be recyclable.

- No vents allowed because they can allow bed bug intrusion.

- Shipped in 4 mil poly bags rolled or flat is acceptable.

Tolerance:

- Commercial tolerances shall apply to all material and dimensions.

Warranties:

- A minimum of two (2) year warranty is acceptable on workmanship and material.   Excluded from this warranty will be misuse of mattress such as burns, chemicals, negligence, or improper cleaning.

Delivery:

- Delivery date no later than 07/17/2024

- Just on time Delivery is required, no early delivery.

- Delivery must be made during regular working hours of 8:00 AM to 4:00 PM

- Delivery Address:

1581 Stadium Road

Brookings SD 57007

- 24-hour notice is requested for delivery.  Bryan Bisson 605-695-7576 or Eric Miner 605-690-8133